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Knowledge Bites

Current Rebar Sales Codes (Regular Production)

	Diameter
	Length
	Material Code
	Family Code
	Grade

	millimetre
	metre
	
	
	

	10
	12
	WR541001200
	B100C
	B500C 

	12
	6
	WR541200600
	B120C
	

	
	12
	WR541201200
	
	

	
	14
	WR541201400
	
	

	16
	6
	WR541600600
	B160C
	

	
	12
	WR541601200
	
	

	
	14
	WR541601400
	
	

	
	15
	WR541601500
	
	

	20
	6
	WR542000600
	B200C
	

	
	12
	WR542001200
	
	

	
	14
	WR542001400
	
	

	
	15
	WR542001500
	
	

	
	16
	WR542001600
	
	

	25
	12
	WR542501200
	B250C
	

	
	14
	WR542501400
	
	

	
	15
	WR542501500
	
	

	
	16
	WR542501600
	
	

	
	18
	WR542501800
	
	

	32
	12
	WR543201200
	B320C
	

	
	14
	WR543201400
	
	

	
	15
	WR543201500
	
	

	
	16
	WR543201600
	
	

	
	17
	WR543201700
	
	

	
	18
	WR543201800
	
	

	40
	12
	WR544001200
	B400C
	

	
	14
	WR544001400
	
	

	
	15
	WR544001500
	
	

	
	16
	WR544001600
	
	

	
	17
	WR544001700
	
	

	
	18
	WR544001800
	
	































Those are the standard production lengths acknowledged by the mill.


[bookmark: _GoBack]The rolling of what is termed long or extender lengths, (the term relates to transport requirements), is planned according to orders placed by the independent market sector and a forecast of requirements by CSS (Group) through to next planned, (anticipated), rolling dates of said diameter.

The mill is practically capable of rolling any lengths to a single decimal place between 6metre & 18metre. For example 10.0metre, 13.5metre, 17.5metre etc...
These ‘non-standard lengths’ are rolled strictly to order.

The mill is also able to roll 50mm diameter strictly to order. 

	Diameter
	Length
	Material Code
	Family Code
	Grade

	millimetre
	metre
	
	
	

	50
	12
	WR545001200
	B500C
	B500C

	
	14
	WR545001400
	
	

	
	15
	WR545001500
	
	

	
	16
	WR545001600
	
	

	
	17
	WR545001700
	
	

	
	18
	WR545001800
	
	



This one diameter can require a significant number of non-standard or make to order lengths within the rolling sequence. 

The Reason? 
Well, a 1.5-metre offcut from a 16mm diameter bar weighs 2.37 kilograms. The same offcut of 50mm diameter weighs 23.1 kilograms, a significant loss in monetary terms.
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